Meterial of main parts

| Part name | Meterial |
| --- | --- |
| Valve body | WCB,QT450-10,Q235,Alloy steel,stainless steel,etc. |
| Valve stem | Alloy steel,stainless steel |
| Seal ring | Stainless steel composite multi-level |
| Packing | Flexible graphite or stuffing |
| Valve seat | Stainless steel,cobalt based hard alloy |
| Valve stem | Stainless steel |